TriboModel
We conducted multi-cycle dry sliding tests using CR7V pin heads against AA6082 aluminium blanks at various temperatures. The mean and std for each cycle during the multi-cycle test is recorded. A critical temperature phenomenon was discovered when the blank temperature was set to 167.5°C. The experimental results revealed three distinct temperature-dependent regimes (under-processed figures attached):

Room temperature (25°C): Limited galling observed, coefficient of friction (COF) remains constant at low values.

165°C: Transient galling observed - COF oscillates, with periodic spikes occurring.

167.5°C: Transient galling became more frequent with more oscillations.

170°C: Permanent galling - COF remains constantly high.

Data can be accessed in corresponding folders.

This temperature sensitivity is remarkable, with only 2.5°C difference causing a fundamental shift in tribological behaviour. The 167.5°C condition appears to represent a critical balance point where galling material repeatedly attaches, accumulates, and detaches in a cyclical pattern.

Based on the data, a simplified physics-based model can be developed to describe the transient galling phenomenon observed in multi-cycle hot forming of AA6082 aluminium alloy. The model captures the temperature-sensitive cyclical behaviour where the coefficient of friction (COF) oscillates between stable low values (~0.2) and high spikes (~1.2) before returning to baseline.

Core Mechanism

The model is based on a mass balance approach for the aluminum transfer layer that accumulates on the pin surface (representing tool asperities) through repeated contact with fresh heated blanks. The key innovation is modeling the competition between:

- Material attachment from the hot blank to the pin

- Natural wear/ejection of the transfer layer

- Detachment events when accumulated material reaches a critical mass

Three Temperature Regimes Explained

- 25 - 165°C: Stable low COF (~0.2) - attachment rate too low to reach critical mass

- 165 - 170°C: Transient galling - attachment and detachment rates are balanced, creating limit cycle oscillations

- 170+°C: Permanent galling - critical mass too high or attachment too strong, material never detaches

Mathematical Formulation

- Transfer Layer Mass Evolution

For Mn< McritT (Accumulation phase):

Mn+1= Mn+ QattachT- Qwearn

For Mn≥ McritT (Detachment event):

Mn+1= α · Mn

Where:

- Mn = transfer layer mass after cycle n

- QattachT = material attachment rate (temperature-dependent)

- Qwearn = natural wear rate

- McritT = critical mass threshold for detachment (temperature-dependent)

- α = retention fraction after detachment (0.1-0.3)

Initial condition: M0= 0 (virgin pin surface)

Physical interpretation: Each cycle, material transfers from the fresh hot blank to the pin. The transfer layer grows through accumulation until it reaches a critical mass, at which point mechanical instability causes large-scale detachment, leaving only a residual layer (α fraction).

- Material Attachment Rate (Temperature-Dependent)

QattachT= k0·expT - TrefT0

Where:

- k0 = baseline attachment rate constant

- Tref = reference temperature = 25°C or higher

- T0 = temperature sensitivity parameter (~20-30°C)

Physical interpretation: Higher temperature → softer aluminium → stronger adhesion → more material transfer from fresh hot blank to pin. The exponential (Arrhenius-type) relationship captures the temperature activation of adhesion processes.

Multi-cycle consideration: Qattach might also depends on the pin's current transfer layer state Mn but is not considered at the moment due to complexity.

- Natural Wear Rate

Qwearn= kw· Mn

Where:

- kw = wear rate constant (0.05-0.15)

Physical interpretation: Wear rate is proportional to current mass - thicker layers experience more mechanical instability, larger contact area for particle ejection.

- Critical Mass for Detachment (Temperature-Dependent with Stochastic Element)

Mean critical mass:

McritT= M0·exp-T - TrefTc

Stochastic critical mass (accounting for experimental variability):

Mcritn, T= McritT· 1 + εn

Where:

- εn ~ Normal(0, σ) is random noise sampled independently each cycle

- M0 = baseline critical mass at reference temperature

- Tc = critical temperature parameter (~40-60°C)

The exponential temperature dependence means that higher temperature leads to higher critical mass:

- Higher temperature → stronger interfacial bonding (enhanced diffusion, metallic bonding)

- Stronger bonding → can support thicker layer before detachment

- At 170°C, Mcrit may be so large that detachment never occurs (permanent galling)

The stochastic component captures real-world variability. Spike intervals vary realistically (e.g., 5, 8, 12, 6, 10 cycles) rather than being perfectly periodic, matching experimental observations.

- Coefficient of Friction (Sigmoid Transformation)

μn=μmin+μmax-μmin· 11 +exp-λ · Mn-McritT2

Where:

- μmin = around 0.2 (stable thin layer)

- μmax = around 1.2 (thick Al-Al cohesive contact)

- λ = transition steepness parameter (3-7)

- McritT2 = inflection point (COF transition occurs at half critical mass)

Physical basis:

This Sigmoid (S-shaped) function captures the smooth, nonlinear transition from low to high friction as the transfer layer accumulates:

- Low M (<Mcrit4): Thin stable layer acts as solid lubricant with third-body particles → μ ≈ μmin

- Medium M (≈Mcrit2): Transition region with increasing Al-Al metallic contact and cohesive forces → rapid COF rise

- High M (>3Mcrit4): Thick layer dominated by strong cohesive Al-Al bonding and plastic deformation → μ ≈ μmax

Next step: determine all parameters using experimental data, then validate the current model.